## Slide 1
Annual Summary of Molten Metal Incidents in 2024
September 2025

## Slide 2
Explosion Rating Force Criteria
TABLE 1. Explosion Rating Force Criteria Sep. 2025
Guidelines | Force 1 | Force 2 | Force 3
Property Damage | None | Minor | Considerable
Light | Minimal | Flash | Intense
Sound | Short cracking | Loud Report | Painful
Vibration | Short and sharp | Brief rolling | Massive structural
Metal Dispersion | <15 feet | >15 to 50 feet | >50 feet
Low
Severe

## Slide 3
FIGURE 1. Incidents Reported For The Period 1981 – 2024 Sep. 2025
Incidents by Year 1981 – 2024 (Total 4834)

## Slide 4
FIGURE 2. Incidents By Force Level 1981 – 2024 Sep. 2025
Incidents by Force Level 1981 – 2024 (Total 4834)

## Slide 5
FIGURE 3. Incidents By Force Levels 2 & 3 For 1981 – 2024 Sep. 2025
Incidents by Force Levels 2 & 3 1981 – 2024

## Slide 6
FIGURE 4. % Reported as Force Levels 1 & 2 For 2000 – 2024 Sep. 2025
% Incidents Reported as Force Levels 1&2 2000 - 2024
Chart: 
| 2000 | 2001 | 2002 | 2003 | 2004 | 2005 | 2006 | 2007 | 2008 | 2009 | 2010 | 2011 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022 | 2023 | 2024
% Force 1 | 0.67857 | 0.72794 | 0.81818 | 0.8125 | 0.69565 | 0.81765 | 0.78512 | 0.71429 | 0.72289 | 0.63492 | 0.83529 | 0.81553 | 0.89655 | 0.92941 | 0.93458 | 0.93678 | 0.90256 | 0.8674 | 0.87059 | 0.8253 | 0.91156 | 0.82857 | 0.88384 | 0.83333 | 0.79433
%Force 2 | 0.28571 | 0.24265 | 0.17576 | 0.15909 | 0.26812 | 0.17059 | 0.19008 | 0.25 | 0.26506 | 0.34921 | 0.16471 | 0.17476 | 0.10345 | 0.070588 | 0.056075 | 0.057471 | 0.092308 | 0.1326 | 0.11765 | 0.16867 | 0.081633 | 0.16429 | 0.11616 | 0.16667 | 0.19149

## Slide 7
FIGURE 5. Force 3 Incidents For 1981 – 2024 Sep. 2025
5 Yr. Avg.: 0.8
10 Yr. Avg: 0.9
2.5
Force 3 Incidents Only 1981 – 2024

## Slide 8
FIGURE 6. Incidents By Force Level 1981 – 2024 Sep. 2025
Incidents by Force Level 1981 – 2024 (Total 4834)

## Slide 9
FIGURE 7. All Force Levels By Percentage 1981 – 2024 Sep. 2025
All Force Levels by Percentage 1981 – 2024

## Slide 10
FIGURE 8. Injuries From Incidents For 1981 – 2024 Sep. 2025
Injuries from Incidents 1981 – 2024 (Total 1686)

## Slide 11
FIGURE 9. % Injuries/Total Annual Incidents 2001 – 2024 Sep. 2025
% Injuries per Total Annual Incidents 2001 – 2024 (Total 877 Injuries)
Chart: 
| 2001 | 2002 | 2003 | 2004 | 2005 | 2006 | 2007 | 2008 | 2009 | 2010 | 2011 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022 | 2023 | 2024
 | 0.38971 | 0.49091 | 0.375 | 0.22464 | 0.25294 | 0.39669 | 1.2054 | 0.57831 | 0.47619 | 0.22353 | 0.34951 | 0.39655 | 0.27059 | 0.28037 | 0.32184 | 0.092308 | 0.044199 | 0.15294 | 0.090361 | 0.047619 | 0.071429 | 0.065657 | 0.10897 | 0.29078

## Slide 12
FIGURE 10. Avg. # Injuries / Yr. For 2001-2016, 2017-2023 & 2024 Sep. 2025
Average # of Injuries / Year from Explosions
Chart: 
| Avg. Fatal /Yr | Avg. Serious / Yr | Avg Minor /Yr. | Avg Total /Yr.
2001-2016 | 2.19 | 7.2 | 36.88 | 46.25
2017-2021 | 1.6 | 1.6 | 10 | 13.2
2024 | 7 | 3 | 31 | 41
% Reduciton ('01-'16 vs '17-'23) | 0.26941 | 0.77778 | 0.72885 | 0.71459

## Slide 13
FIGURE 11. Injuries By Severity For 1981 – 2024 Sep. 2025
Injuries by Severity – Total 1686 1981 – 2024

## Slide 14
FIGURE 12. Injuries Levels By Percentage For 1981 – 2024 Sep. 2025
Injury Levels by Percentage 1981 - 2024

## Slide 15
FIGURE 13. Injury Risk Per 100 Explosions For 1981 – 2024 Sep. 2025
Injury Risk per 100 Explosions 1981 - 2024

## Slide 16
FIGURE 14. Fatalities From Explosions For 1981 – 2024 Sep. 2025
Avg # Fatals Last 10 Yrs – 1.5
Fatalities from Explosions 1981 - 2024

## Slide 17
FIGURE 15. Force Level Incidents By Operation For 2024 Sep. 2025
Force Level Incidents by Operation – 2024

## Slide 18
FIGURE 16. Force Level & % Incidents By Operation For 1980 – 2024 Sep. 2025
68%
27%
5%
81%
18%
1%
81%
90%
8%
2%
18%
1%
Force Level & % Incidents by Operation
1980 – 2024

## Slide 19
FIGURE 17. Melting Injuries and Incidents 1990 – 2024 Sep. 2025
Melting Injuries and Incidents
1990 – 2024 (Total 335 Injuries)
Chart: 
| 1990 | 1991 | 1992 | 1993 | 1994 | 1995 | 1996 | 1997 | 1998 | 1999 | 2000 | 2001 | 2002 | 2003 | 2004 | 2005 | 2006 | 2007 | 2008 | 2009 | 2010 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022 | 2023 | 2024
Melting Injuries | 20 | 6 | 8 | 24 | 25 | 6 | 6 | 21 | 1 | 12 | 4 | 8 | 10 | 6 | 14 | 6 | 8 | 91 | 10 | 3 | 1 | 0 | 1 | 1 | 37 | 0 | 2 | 1 | 1 | 1 | 0 | 0 | 1 | 0
Melting Incidents | 54 | 35 | 38 | 67 | 42 | 42 | 25 | 27 | 29 | 22 | 56 | 45 | 42 | 35 | 40 | 39 | 31 | 27 | 27 | 14 | 20 | 14 | 27 | 31 | 51 | 39 | 68 | 46 | 65 | 55 | 55 | 74 | 42 | 29

## Slide 20
FIGURE 18. Melting Injuries Per Incidents 1990 – 2024 Sep. 2025
Melting Injuries per Incidents
1990 – 2024
Chart: 
| 1990 | 1991 | 1992 | 1993 | 1994 | 1995 | 1996 | 1997 | 1998 | 1999 | 2000 | 2001 | 2002 | 2003 | 2004 | 2005 | 2006 | 2007 | 2008 | 2009 | 2010 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022 | 2023 | 2024
Melting Injuries / Incident | 0.37037 | 0.17143 | 0.21053 | 0.35821 | 0.59524 | 0.14286 | 0.24 | 0.77778 | 0.034483 | 0.54545 | 0.071429 | 0.17778 | 0.2381 | 0.17143 | 0.35 | 0.15385 | 0.25806 | 3.3704 | 0.37037 | 0.21429 | 0.05 | 0 | 0.037037 | 0.032258 | 0.72549 | 0 | 0.029412 | 0.021739 | 0.015873 | 0.018182 | 0 | 0 | 0.02381 | 0
2007 Rate – 3.4 Due to Force 3 China Explosion w/ 84 Total Injuries, Including 16 Fatalities

## Slide 21
FIGURE 19. Casting Injuries and Incidents 1990 – 2024 Sep. 2025
Casting Injuries and Incidents
1990 – 2024 (Total 394 Injuries)
Chart: 
| 1990 | 1991 | 1992 | 1993 | 1994 | 1995 | 1996 | 1997 | 1998 | 1999 | 2000 | 2001 | 2002 | 2003 | 2004 | 2005 | 2006 | 2007 | 2008 | 2009 | 2010 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022 | 2023 | 2024
Casting Injuries | 20 | 15 | 4 | 7 | 9 | 12 | 9 | 16 | 27 | 18 | 20 | 19 | 17 | 10 | 6 | 8 | 15 | 20 | 13 | 15 | 6 | 4 | 0 | 6 | 2 | 14 | 1 | 16 | 8 | 3 | 8 | 10 | 5 | 31
Casting Incidents | 55 | 28 | 29 | 19 | 22 | 29 | 21 | 17 | 19 | 22 | 44 | 30 | 38 | 57 | 44 | 58 | 36 | 45 | 23 | 20 | 30 | 24 | 32 | 31 | 76 | 116 | 75 | 71 | 62 | 66 | 59 | 93 | 63 | 71

## Slide 22
FIGURE 20. Casting Injuries Per Incidents 1990 – 2024 Sep. 2025
Casting Injuries per Incidents
1990 – 2024
Chart: 
| 1990 | 1991 | 1992 | 1993 | 1994 | 1995 | 1996 | 1997 | 1998 | 1999 | 2000 | 2001 | 2002 | 2003 | 2004 | 2005 | 2006 | 2007 | 2008 | 2009 | 2010 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022 | 2023 | 2024
Casting Injuries / Incident | 0.36364 | 0.53571 | 0.13793 | 0.36842 | 0.40909 | 0.41379 | 0.42857 | 0.94118 | 1.4211 | 0.81818 | 0.45455 | 0.63333 | 0.44737 | 0.17544 | 0.13636 | 0.13793 | 0.41667 | 0.44444 | 0.56522 | 0.75 | 0.2 | 0.16667 | 0 | 0.19355 | 0.026316 | 0.12069 | 0.013333 | 0.22535 | 0.13115 | 0.047619 | 0.13559 | 0.108 | 0.079365 | 0.43662

## Slide 23
FIGURE 21. Transfer Injuries and Incidents 1990 – 2024 Sep. 2025
Transfer Injuries and Incidents
1990 – 2024 (Total 264 Injuries)
Chart: 
| 1990 | 1991 | 1992 | 1993 | 1994 | 1995 | 1996 | 1997 | 1998 | 1999 | 2000 | 2001 | 2002 | 2003 | 2004 | 2005 | 2006 | 2007 | 2008 | 2009 | 2010 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022 | 2023 | 2024
Transfer Injuries | 3 | 8 | 0 | 0 | 3 | 13 | 13 | 4 | 6 | 9 | 12 | 17 | 34 | 22 | 4 | 18 | 13 | 10 | 16 | 8 | 2 | 2 | 0 | 7 | 3 | 0 | 3 | 8 | 4 | 3 | 2 | 3 | 10 | 4
Transfer Incidents | 13 | 8 | 11 | 16 | 8 | 15 | 14 | 17 | 11 | 18 | 36 | 45 | 60 | 48 | 34 | 50 | 36 | 23 | 20 | 18 | 20 | 3 | 5 | 27 | 20 | 18 | 23 | 40 | 23 | 19 | 22 | 21 | 42 | 32

## Slide 24
FIGURE 22. Transfer Injuries Per Incidents 1990 – 2024 Sep. 2025
Transfer Injuries per Incidents
1990 – 2024
Chart: 
| 1990 | 1991 | 1992 | 1993 | 1994 | 1995 | 1996 | 1997 | 1998 | 1999 | 2000 | 2001 | 2002 | 2003 | 2004 | 2005 | 2006 | 2007 | 2008 | 2009 | 2010 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022 | 2023 | 2024
Transfer Injuries / Incident | 0.23077 | 1 | 0 | 0 | 0.375 | 0.86667 | 0.92857 | 0.23529 | 0.54545 | 0.5 | 0.33333 | 0.37778 | 0.56667 | 0.45833 | 0.11765 | 0.36 | 0.36111 | 0.43478 | 0.8 | 0.44444 | 0.1 | 0.66667 | 0 | 0.25926 | 0.15 | 0 | 0.13043 | 0.2 | 0.17391 | 0.15789 | 0.090909 | 0.14286 | 0.2381 | 0.125

## Slide 25
FIGURE 23. Melting Explosions By Cause For 2024 Sep. 2025
Major Causes
Wet & Oxidized: Scrap, Sows, RSI
Wet / Oxidized Alloy Additions: Si, Cu, Flux
Wet Equipment
29 Melting Explosions – 2024

## Slide 26
FIGURE 24. Melting Explosions By Charge Material 1980 – 2024 Sep. 2025
Melting Explosions – Charge Material Involved
1980 – 2024

## Slide 27
FIGURE 25. Casting Explosions For 2024 Sep. 2025
2 Force 1 – Roll Casting
71 Casting Explosions – 2024

## Slide 28
FIGURE 26. Casting Explosions By Cast Segment 1980 – 2024 Sep. 2025
DC/HDC/EMC Explosions by Cast Segment
1980 – 2024

## Slide 29
FIGURE 27. Major Causes of Casting Incidents For 2024 Sep. 2025
DC Start-up Issues: Wet Starting Blocks / Wet Equipment / Butt Curl –Bleed-outs
DC Steady State Issues: Equipment Failure / Operator Error
DC Termination Issues: Wet / Rusty Drain Pan / Wet Hand Tool / Ingot Head Under Water
Strip / Roll Casting: Start-up Wet Unoiled Drain Pan
Sow / Mold Casting Issues: Wet / Unpreheated / Cracked Molds; Wet Hand Tool
Major Causes of 71 Casting Incidents – 2024

## Slide 30
FIGURE 28. Casting Explosions by Major Causes 2015 – 2024 Sep. 2025
Major Causes of Casting Explosions
2015 – 2024
Chart: 
| Sow Casting - Wet / Cracked / Rusty Molds | DC Cast Start - Excessive Curl / Hang-up / Bleed-out | End of DC Cast & Aborts - Wet / Rusty Drain Pan | Wet Refractory or Equipment | Equipment Failure / Maint. Issue / Set-up | DC Cast Start - Wet / Rusty Bottom Block | Ingot Head Under Water | SOP Unadapted or Unrespected





 | 258 | 69 | 64 | 53 | 48 | 40 | 13 | 6

## Slide 31
FIGURE 29. Casting Explosions by Major Causes 2015 – 2024 Sep. 2025
Major Causes of Force 2 & 3 Casting Explosions
2015 – 2024
Chart: 
| End of DC Cast & Aborts - Wet / Rusty Drain Pan | DC Cast Start - Excessive Curl / Hang-up / Bleed-out | Sow Casting - Wet / Cracked / Rusty Molds | DC Cast Start - Wet / Rusty Bottom Block | Equipment Failure / Maint. Issue | Ingot Head Under Water | Wet Refractory or Equipment





 | 22 | 19 | 13 | 11 | 6 | 3 | 3

## Slide 32
FIGURE 30. Causes of Transfer Explosions For 2024 Sep. 2025
Major Causes of 32 Transfer Explosions – 2024
14 - Wet Hand or Furnace Tools, Equipment
6 – Wet / Rusty Drain or Skim Pan (1 Force 2)
4 – Wet Launder Refractory
4 – Wet Sampling Molds
2 – Metal on Floor

## Slide 33
FIGURE 31. Transfer Explosions by Equipment 1980 – 2024 Sep. 2025
Transfer Explosions by Equipment
1980 – 2024 (Total 938)

## Slide 34
FIGURE 32. Transfer Explosions – Major Causes 2008 – 2024 Sep. 2025
Major Causes of Transfer Explosions
2008 – 2024 (w/o 2011)
Chart: 
| Wet / Rusty Drain Pan | Wet Tools | Wet Refractory or Equipment | Wet Floor / Spill
 | 154 | 144 | 106 | 27

## Slide 35
FIGURE 33. Transfer Explosions – Major Causes 2008 – 2024 Sep. 2025
Major Causes of Force 2 & 3 Transfer Explosions
2008 – 2024 (w/o 2011)
Chart: 
| Wet / Rusty Drain Pan | Wet Refractory or Equipment | Wet Floor / Spill
 | 19 | 9 | 5

## Slide 36
FIGURE 34. Injuries By Operation For 2024 Sep. 2025
41 Injuries by Operation – 2024

## Slide 37
FIGURE 35. Injuries By Operation For 1980 – 2024 Sep. 2025
1693 Injuries by Operation:
1980 – 2024

## Slide 38
FIGURE 36. Force Level By Process Plant Reported For 2024 Sep. 2025
Force Level By Process Plant – 2024

## Slide 39
FIGURE 37. Force Level By Process Plant Reported For 1980 – 2024 Sep. 2025
Force Level By Process Plant
1980 – 2024

## Slide 40
FIGURE 38. Reduction Plant Incidents Summary 2024 Sep. 2025
Melting Incidents | Casting Incidents
4 – Wet Charge: Scrap (Force 2) 2 – Contaminated Alloy: Si | Small Mold & Sow Casting: 27 – Cracked, Wet or Rusty Molds (3 – Force 2) 1 – Wet Hand Tool
 | VDC – Slab 3 –Start-up – Wet Equip. / Hand Tool 1 – Start-up – Excess Curl VDC – Billet 2 –Start-up – Wet Equip. / Hand Tool
Reduction Plant
Main Causes of 64 Incidents – 2024

## Slide 41
FIGURE 39. Reduction Plant Incidents Summary 2024 Sep. 2025
Transfer Incidents | Reduction Cell
7 – Wet Hand Tools 4 – Wet Sampler Molds 3 –Wet Refractory / Transfer Troughs – 2 – Tap Out – Wet Floor 2 – Siphoning – Wet Equipment 1 – Wet Ladle 1 – Wet / Rusty Drain Pan | 2 – Wet Anode 2 – Wet Pot Addition 2 – Wet Wood 1 – Tap-out - Wet Floor 1 – Wet Equipment
Reduction Plant
Main Causes of 64 Incidents – 2024

## Slide 42
FIGURE 40. Recycling Plant Incidents Summary 2024 Sep. 2025
Melting Incidents | Casting Incidents
4 - Wet Charge: Scrap (2 - Force 2) | VDC – Billet: 1 – Stead State – Cable Failure (Force 3) VDC – Slab: 2 - Start-up – Bleedout (Force 2) 1 - Start-up – Wet Bottom Block 1 – Termination – Wet Tool (Force 2) 1 – Termination – Molten on Wet Ingot Head (Force 2)
Transfer Incidents 1 - Wet Trough 1- Wet Skim Pan | 
Recycling Plant
Main Causes of 12 Incidents – 2024

## Slide 43
FIGURE 41. Reduction Plant Injuries By Operation 2024 Sep. 2025
5 – Minor Injuries
3 – Wet Tool
2 – Wet Additions
(Reduction Process)
Reduction Plant Injuries & Incident Causes – 2024

## Slide 44
FIGURE 42. Rolling Plant Injuries By Operation 2024 Sep. 2025
3 -Start-Abort – Wet Drain Pan
1 – Start – Excess Curl
1 – start – Wet Bottom Block
2 – Term. Wet Drain Pan
2 - Term. Ingot Head Under H2O
3- Lancing – Wet Floor
Rolling Plant Injuries & Incident Causes - 2024

## Slide 45
FIGURE 43. Extrusion Plant Injuries By Operation 2024 Sep. 2025
2 Fatal & 1 Serious – VDC Steady State – Operator Error - High Cast Rate
Extrusion Plant Injuries & Incident Cause – 2024

## Slide 46
FIGURE 44. Recycling Plant Injuries By Operation 2024 Sep. 2025
5 Fatal & 14 Minor – VDC Steady State Equip. Failure
1 Minor – VDC Termination - Wet Tool
Recycling Plant Injuries & Incident Causes – 2024

## Slide 47
FIGURE 45. Injury Severity By Process Plant – 2024 Sep. 2025
Injury Severity by Process Plant – 2024
1 Other: R&D Transfer – Wet Equipment

## Slide 48
FIGURE 46. Injuries Severity By Plant Reported For 1980 – 2024 Sep. 2025
Injury Severity by Process Plant
1980 – 2024

## Slide 49
FIGURE 47. Reduction & Recycling Incident, Injury & Injury Rate 2012-2024 Sept. 2025
Reduction & Recycling Plant Incidents, Injuries / Incident Rate
2012 – 2024
Chart: Reduction Plant
| 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022 | 2023 | 2024
Incidents | 40 | 55 | 78 | 119 | 139 | 84 | 87 | 51 | 66 | 50 | 78 | 84 | 64
Injuries | 19 | 20 | 21 | 49 | 6 | 5 | 7 | 4 | 2 | 2 | 6 | 11 | 5
Injury/ Incident Rate | 0.475 | 0.36364 | 0.26923 | 0.41176 | 0.043165 | 0.059524 | 0.08046 | 0.078431 | 0.030303 | 0.04 | 0.076923 | 0.13095 | 0.078125
Chart: Recycling Plant
| 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022 | 2023 | 2024
Incidents | 7 | 8 | 4 | 6 | 9 | 42 | 21 | 44 | 31 | 37 | 49 | 21 | 12
Injuries | 0 | 0 | 0 | 0 | 1 | 0 | 1 | 2 | 0 | 2 | 0 | 1 | 20
Injury/ Incident Rate | 0 | 0 | 0 | 0 | 0.11111 | 0 | 0.047619 | 0.045455 | 0 | 0.054054 | 0 | 0.047619 | 1.6667

## Slide 50
FIGURE 48. Rolling & Extrusion Incident, Injury & Injury Rate 2012-2024 Sept. 2025
Rolling & Extrusion Plant Incidents, Injuries / Incident Rate
2012 – 2024
Chart: Roling Plant
| 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022 | 2023 | 2024
Incidents | 9 | 10 | 11 | 36 | 36 | 44 | 47 | 58 | 38 | 31 | 46 | 36 | 52
Injuries | 2 | 1 | 4 | 4 | 6 | 2 | 5 | 5 | 3 | 4 | 6 | 2 | 12
Injury/ Incident Rate | 0.22222 | 0.1 | 0.36364 | 0.11111 | 0.16667 | 0.045455 | 0.10638 | 0.086207 | 0.078947 | 0.12903 | 0.13043 | 0.055556 | 0.23077
Chart: Extrusion Plant
| 2012 | 2013 | 2014 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022 | 2023 | 2024
Incidents | 2 | 8 | 13 | 11 | 10 | 15 | 10 | 6 | 18 | 25 | 16 | 12
Injuries | 1 | 1 | 3 | 5 | 0 | 13 | 0 | 2 | 2 | 1 | 3 | 3
Injury/ Incident Rate | 0.5 | 0.125 | 0.23077 | 0.45455 | 0 | 0.86667 | 0 | 0.33333 | 0.11111 | 0.04 | 0.1875 | 0.25

## Slide 51
Thank you!
@AluminumNews | @ChooseAluminum | @DriveAluminum
Aluminum.org
JOIN THE CONVERSATION